### Cement Tiles Description

Our cement tiles are meticulously handcrafted by skilled artisans in Mexico, ensuring each tile is unique and of the highest quality. Made from a blend of natural materials, including cement, sand, and mineral pigments, our tiles are durable, environmentally friendly, and designed to add beauty and character to any space.

### Key Features

- Handmade Craftsmanship: Each tile is individually crafted, ensuring unique patterns and high-quality finishes.

- Durability: Our cement tiles are built to withstand heavy foot traffic and resist wear and tear, making them perfect for both residential and commercial applications.

- Versatility: Suitable for a variety of applications, including floors, walls, countertops, and outdoor spaces.

- Eco-Friendly: Made from natural materials and pigments, our tiles are an environmentally responsible choice.

- Customizable: Available in a wide range of colors, patterns, and sizes, and can be customized to meet your specific design needs.

### Specifications

- Material Composition: Cement, marble powder, sand, mineral pigments

- Tile Size Options:

  - Standard sizes: 8x8x5/8 inches (20x20x1.6 cm), 12x12x6/8 inches (30x30x2 cm)

  - Custom sizes available upon request

- Thickness: Approximately 5/8 inch (1.6 cm) (8×8 size) (also available in 3/8 inch)

- Color layer: Approximately (3 to 4 mm)

- Weight: Approximately 3 lbs per tile (8×8 size) (1.3 Kgs)

- Surface Finish: Matte or polished

- Color Options: Wide range of colors available; custom colors can be created

- Pattern Options: Extensive selection of patterns, including geometric, floral, and custom designs

- Installation: Suitable for indoor and outdoor use; must be sealed after installation

- Note: Size, Thickness, Color, Weight may vary due to the handmade process.

### Technical Information

- Water Absorption: <10% (9.5 to 10.5%)

- Compressive Strength: ≥ 20 MPa

- Flexural Strength: ≥ 7 MPa

- Abrasion Resistance: High resistance to wear, suitable for high-traffic areas

  - 3 to 4 Mohs – approximately same as Black Marble

- Thermal Resistance: Suitable for use with underfloor heating systems

- Average Coefficient of Friction:

  - Unpolished dry: 0.88 – Polished dry: 0.83

  - Unpolished wet: 0.92 – Polished wet: 0.68

- Freeze / Thaw Resistance: Like concrete, untreated cement tiles are not resistant to freeze / thaw cycles and should be protected with penetrating sealer and a second coat of a sealer based in acrylic.

- Acid Resistance: Cement tiles are not resistant to acids and should be cleaned with pH neutral cleaners.

- Use in Wet areas: A high quality effective sealant must be used for shower, spa, or pool use.

### Tiles Tests results by the Tile Council of North America (TCNA), report TCNA-576-12

- ANSI A137.1-2012: Wet Dynamic Coefficient of Friction (DCOF) | Average 0.65

- ASTM C1028: Static Coefficient of Friction (SCOF) | Average Dry 0.85 – Wet 0.78

- ASTM C648-04: Standard Breaking Strength | Average 789 lbf

- ASTM C373: Standard Water Absorption | Average 14.94% (without sealer)

### Applications

- Residential: Ideal for kitchens, bathrooms, living rooms, and patios

- Commercial: Perfect for restaurants, hotels, retail spaces, and office buildings

- Custom Projects: Can be tailored to meet specific design and architectural requirements

### Maintenance

- Cleaning: Clean with a pH-neutral cleaner and a soft cloth or mop. Avoid harsh chemicals and abrasive materials.

- Sealing: Apply a high-quality sealant after installation to protect against stains and moisture. Reapply sealant periodically based on usage and exposure to elements.

- Repairs: In the event of damage, individual tiles can be replaced.

### Key Features

- Handmade Craftsmanship: Each tile is individually crafted, ensuring unique patterns and high-quality finishes.

- Durability: Our cement tiles are built to withstand heavy foot traffic and resist wear and tear, making them perfect for both residential and commercial applications.

- Versatility: Suitable for a variety of applications, including floors, walls, countertops, and outdoor spaces.

- Eco-Friendly: Made from natural materials and pigments, our tiles are an environmentally responsible choice.

- Customizable: Available in a wide range of colors, patterns, and sizes, and can be customized to meet your specific design needs.

### Specifications

- Material Composition: Cement, marble powder, sand, mineral pigments

- Tile Size Options:

  - Standard sizes: 8x8x5/8 inches (20x20x1.6 cm), 12x12x6/8 inches (30x30x2 cm)

  - Custom sizes available upon request

- Thickness: Approximately 5/8 inch (1.6 cm) (8×8 size) (also available in 3/8 inch)

- Color layer: Approximately (3 to 4 mm)

- Weight: Approximately 3 lbs per tile (8×8 size) (1.3 Kgs)

- Surface Finish: Matte or polished

- Color Options: Wide range of colors available; custom colors can be created

- Pattern Options: Extensive selection of patterns, including geometric, floral, and custom designs

- Installation: Suitable for indoor and outdoor use; must be sealed after installation

- Note: Size, Thickness, Color, Weight may vary due to the handmade process

### Technical Information

- Water Absorption: <10% (9.5 to 10.5%)

- Compressive Strength: ≥ 20 MPa

- Flexural Strength: ≥ 7 MPa

- Abrasion Resistance: High resistance to wear, suitable for high-traffic areas

  - 3 to 4 Mohs – approximately same as Black Marble

- Thermal Resistance: Suitable for use with underfloor heating systems

- Average Coefficient of Friction:

  - Unpolished dry: 0.88 – Polished dry: 0.83

  - Unpolished wet: 0.92 – Polished wet: 0.68

- Freeze / Thaw Resistance: Like concrete, untreated cement tiles are not resistant to freeze / thaw cycles and should be protected with penetrating sealer and a second coat of a sealer based in acrylic.

- Acid Resistance: Cement tiles are not resistant to acids and should be cleaned with pH neutral cleaners.

- Use in Wet areas: A high-quality effective sealant must be used for shower, spa, or pool use.

### Tiles Tests results by the Tile Council of North America (TCNA), report TCNA-576-12

- ANSI A137.1-2012: Wet Dynamic Coefficient of Friction (DCOF) | Average 0.65

- ASTM C1028: Static Coefficient of Friction (SCOF) | Average Dry 0.85 – Wet 0.78

- ASTM C648-04: Standard Breaking Strength | Average 789 lbf

- ASTM C373: Standard Water Absorption | Average 14.94% (without sealer)

### Applications

- Residential: Ideal for kitchens, bathrooms, living rooms, and patios

- Commercial: Perfect for restaurants, hotels, retail spaces, and office buildings

- Custom Projects: Can be tailored to meet specific design and architectural requirements

### Maintenance

- Cleaning: Clean with a pH-neutral cleaner and a soft cloth or mop. Avoid harsh chemicals and abrasive materials.

- Sealing: Apply a high-quality sealant after installation to protect against stains and moisture. Reapply sealant periodically based on usage and exposure to elements.

- Repairs: In the event of damage, individual tiles